## Slide 1: Automated Detection of Tow-Gap Defects in Cross-Ply Composites
Authors: Ahmad Ravangard, Nathan Sage, Aamr Ibrahim
Date: December 7, 2025
A computer-vision pipeline for identifying and characterizing tow-gap defects in AFP laminates.

## Slide 2: Why Tow-Gap Detection Matters
- Tow-gaps reduce fiber volume fraction, introducing resin-rich pockets and weakening mechanical performance.
- Research shows significant decreases in compressive & tensile strength when tow-gaps are present.
- Manual inspection is slow and inconsistent—automated, real‑time inspection is needed.

## Slide 3: Computer Vision for AFP Inspection
- Enables real-time, inline monitoring during manufacturing.
- Reduces operator variability and risk of overlooked defects.
- Deep learning systems detect sub‑millimeter defects at production speeds.
- 3D methods and synthetic data further increase robustness.

## Slide 4: Methodology Overview
- Images divided into 512×512 patches to balance context and detail.
- Tow gaps polygon‑annotated in LabelMe, converted to pixel-accurate masks.
- Dataset includes both defective and defect‑free tiles.
- Augmentations: rotation, perspective, lighting, contrast adjustments.

## Slide 5: Model Summary & Performance
- Lightweight UNet with ResNet34 encoder.
- Metrics: IoU, Dice/F1, Precision, Recall, geometric accuracy.
- Achieved 97% true‑positive rate.
- Fast enough for near real‑time AFP inspection.